HiFive-Unleashed Case Printing Notes:

Case Top and Bottom:
 The HiFive case was designed to be printed in with a large size nozzle, all features are sized for multiple passes with up to a 1.2mm nozzle. The case body has been tested with PLA, ABS and PC-Max, but should work with any rigid material.

Here are the settings that work well with PC-Max and a 1.2mm nozzle (LulzBot® LongBlock):
- Hotend temp: 260C
- Bed temp: 80C
- Gluestick on bed
- Retraction extra prime amount: 2mm^3
- Layer height: 0.6mm
- Wall thickness: 2.4mm
- Infill: 20%

Clips
There are 2 versions of the clips, one for rigid materials and another for semi-flexible materials like nylon, semiflex or some petg’s.

You can also print the design for flexible materials from any rigid material by using a smaller nozzle size (0.4-0.8mm) and vase mode (no top or bottom layers or infill).

Here are the settings that work well with PC-Max and a 1.2mm nozzle (LulzBot® LongBlock):
- Clip for rigid materials
- Hotend temp: 260C
- Bed temp: 80C
- Gluestick on bed
- Retraction extra prime amount: 2mm^3
- Layer height: 0.6mm
- Wall thickness: 2.4mm
- Infill: 60%