Part: moar-printable-LCD-shell-back

Printer: Lulzbot TAZ 6 MOARstruder

Material: PC-max Polymaker

Time: 2 hour, 31 min

Other: glue stick used on bed; zig zag patten for infill, top and bottom layers; extra wall; no skirt

The bottom layer looks great. It’s nice and smooth, though a tad uneven, which may be due to uneven application of glue. I tend to apply more to the corners and edges to prevent warping, but it is noticeable in the final product. Aesthetically it looks acceptable, at least to me.

The biggest issue in the final product is the bottom two holes on the bottom tabs. They aren’t fully printed and probably can’t hold in pips. The second issue is how messy and uneven the top layer is. Most of it looks okay, but along the top of the print it just looks like the printer just globed on the filament, giving the sections raised lines. This makes screwing on the lcd-shell-front piece impossible, as the two pieces won’t flatten together. I’m guessing this is a printer issue, and the only solution I can think of is to use a flat heating tool to flatten it out.

Aside from the two holes on the bottom tabs, all the holes look acceptable, and appear to be okay for putting in the pips. I won’t bother with this print as I won’t be able to screw on the front piece regardless. Next print I will try concentric infill on the top and bottom layers.