Part: moar-printable-LCD-shell-front

Printer: Lulzbot TAZ 6 MOARstruder

Material: PC-max Polymaker

Time: 39min

Other: glue stick used on bed; zig zag patten for infill, top and bottom layers; extra wall; no skirt

The first initial layer looks good, though it is slightly uneven in the application. This may be due to the application of glue onto the bed.

The final product is functional. It lays flat on a surface, but the top layer just looks messy. I’m not sure why the walls are nice, even and smooth, but the zig zag pattern is raised up and uneven. It looks passable along the bottom of it, but in between the holes it just doesn’t look good. Next print I will use the concentric pattern.

The holes are another issue. 10 of the 13 screw holes are filled in and would require a pointy hot end to open them up. Earlier prints with the Aerostruder, all of the holes were open enough to be used, with only occasionally needing a hot end to open a hole more.

The biggest issue is the top layer, which is what the customer would be looking at. It’s uneven, looks messy, and just doesn’t look good aesthetically. I want to try printing it again with a concentric top and and bottom layers to see if there will be a difference.